## Slide 1
INDUSTRIAL FLUOROPOLYMER SOURCING
Pure-Flon Fluoropolymer Tubing Catalog
Use this catalog to shortlist PTFE, PFA, FEP, flexible hose, fittings, and spaghetti tubing before sending an RFQ through pure-flon.com/quote.
PTFE / PFA
65 deg C - 260 deg C
FEP
65 deg C - 205 deg C
RFQ
pure-flon.com/quote
Buyer-ready reference for tubing, hose, fittings, dimensions and quote preparation.
Release 2026-06-03
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
1

## Slide 2
RFQ WORKFLOW
Move buyers from interest to a useful technical brief.
The catalog should reduce clarification loops by asking for environment first, then material and dimensions.
Buyer action
What to prepare
Pure-Flon review output
Shortlist material
Media, temperature, pressure, transparency, static and clean-handling needs.
Material family recommendation and constraints to verify.
Confirm dimensions
ID, OD, wall thickness, tolerance target, bend radius and length.
Metric or inch sizing review plus manufacturing feasibility notes.
Request quote
Application environment, quantity, preferred lead time and destination country.
RFQ response path through pure-flon.com/quote.
Do not start with a generic catalog request. Ask for a short environment-first note and route to quote.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
2

## Slide 3
MATERIAL MAP
Five sourcing buckets cover the early buying decision.
Family
Best-fit sourcing signal
Temp. window
Buyer note
PTFE Tubing
Chemical resistance, broad heat resistance and low-friction service.
65 deg C - 260 deg C
Use when durability matters more than visual flow inspection.
PFA Tubing
High transparency, purity and high-temperature chemical routing.
65 deg C - 260 deg C
Use when visible clean flow and resistance are both important.
FEP Tubing
Transparent non-stick routing with a lower upper temperature range.
65 deg C - 205 deg C
Use for visual checks, low adhesion and moderate heat windows.
Flexible Hose
Assembly paths with bend, routing and pressure review.
Application-dependent
Send bend radius, pressure and connection constraints.
Fittings & Accessories
Connector matching, assemblies and system compatibility.
Application-dependent
Send tube dimensions, media and connection method.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
3

## Slide 4
TUBE FAMILIES
PTFE, PFA and FEP answer different inspection and heat constraints.
PTFE Tubing
Chemical resistance and heat stability
Reference operating temperature window: 65 deg C - 260 deg C.
Core advantages: chemical resistance, heat resistance, low friction and electrical insulation.
Best-fit formats: metric tubing, inch tubing, spaghetti tubing and application-specific wall ranges.
PFA Tubing
High transparency and resistance
Reference operating temperature window: 65 deg C - 260 deg C.
Useful for high-purity chemical routing when visible clean flow matters.
Start here when visual inspection and demanding thermal service both matter.
FEP Tubing
Non-stick and versatile routing
Reference operating temperature window: 65 deg C - 205 deg C.
Useful for visual checks, non-stick surfaces and moderate operating temperature.
Use as a practical transparent option where PFA's upper heat range is not required.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
4

## Slide 5
PRECISION SMALL BORE
PTFE spaghetti tubing gives buyers exact shortlist dimensions.
Outer diameter
Inner diameter
Thickness
Tolerance
0.8 mm
0.3 mm
0.25T
0.05 mm
1.0 mm
0.5 mm
0.25T
0.05 mm
1.3 mm
0.8 mm
0.25T
0.05 mm
1.5 mm
1.0 mm
0.25T
0.05 mm
2.0 mm
1.5 mm
0.25T
0.05 mm
2.5 mm
2.0 mm
0.25T
0.05 mm
Use case: insulation, compact routing, precision tolerance, and early custom-size feasibility checks.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
5

## Slide 6
METRIC PRESSURE REFERENCE
Metric PTFE/PFA rows include pressure, tolerance and bend-radius signals.
OD mm
ID mm
Burst kgf/cm2
Working kgf/cm2
Tol. mm
Min bend radius mm
4
2
120
98
0.15
10
4
2.5
100
80
0.15
13
6
4
65
52
0.15
25
8
6
45
36
0.15
45
10
8
35
28
0.20
70
12
10
30
24
0.20
105
14
12
24
19
0.20
140
16
14
18
14
0.30
140
Safety factor 4:1. Virgin PTFE/PFA. High-precision extrusion reference.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
6

## Slide 7
INCH PRESSURE REFERENCE
Inch-system buyers can match equipment, fittings and maintenance inventory.
OD inch
Wall
OD mm
ID mm
Burst
Working
Tol.
Min bend radius
1/4
1.2T
6.35
3.96
120
98
0.2
25
3/8
1.5T
9.5
6.5
100
80
0.2
40
1/2
1.5T
12.7
9.7
65
52
0.2
105
3/4
1.5T
19
16
45
36
0.3
120
1
1.5T
25.4
22.4
35
28
0.3
430
Pressure values are reference inputs at 23 deg C and can decrease as operating temperature rises. Reference standards: ASTM D3295 PTFE and ASTM D3307 PFA where applicable.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
7

## Slide 8
ASSEMBLY PATH
Hose, fittings and accessories should start from routing constraints.
Path
What to send
Review result
Flexible hose
Routing geometry, bend radius, pressure, media and connection method.
Material and assembly feasibility path.
Fittings
Tube OD/ID, thread or connection type, media and operating temperature.
Compatible fitting or accessory recommendation.
Assembly discussion
Destination country, quantity, lead time and inspection needs.
RFQ-ready clarification set.
Include tube OD/ID, connection method, media, temperature, target country and inspection needs.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
8

## Slide 9
CONTACT FLOW
The quote form should receive a complete technical brief.
Required input
Example detail
Application environment
Chemical media, operating temperature, pressure and duty cycle.
Dimensional target
ID, OD, wall thickness, tolerance, length, bend radius and quantity.
Material signal
PTFE, PFA, FEP, hose, fitting or unclear; Pure-Flon can help shortlist.
Quality and handling
Clean handling, packaging, transparency, static control or inspection requirement.
Commercial route
Country, target date, sample need and preferred reply email.
Next step
Send the RFQ through pure-flon.com/quote and include the checklist details above.
Pure-Flon Fluoropolymer Tubing Catalog - RFQ reference, 2026-06-03
9